GROWTH AND CHARACTERIZATION OF TERNARY CHALCOGENIDE THIN FILMS FOR EFFICIENT SOLAR CELLS AND POSSIBLE INDUSTRIAL APPLICATIONS

By

CHIDI CHUKWUEMEKA UHUEGBU

MATRIC NO: CU03GP0037

A THESIS SUBMITTED IN THE DEPARTMENT OF PHYSICS TO THE SCHOOL OF POSTGRADUATE STUDIES

IN PARTIAL FULFILMENT OF THE REQUIREMENT FOR THE AWARD OF DOCTOR OF PHILOSOPHY OF COVENANT UNIVERSITY, OTA OGUN STATE NIGERIA

JULY, 2007

GROWTH AND CHARACTERIZATION OF TERNARY CHALCOGENIDE THIN FILMS FOR EFFICIENT SOLAR CELLS AND POSSIBLE INDUSTRIAL APPLICATIONS

By

CHIDI CHUKWUEMEKA UHUEGBU

MATRIC NO: CU03GP0037

A thesis submitted in partial fulfillment of the requirements for the award of the degree of Doctor of Philosophy (Ph.D.) in the Department of Physics

Covenant University Ota Nigeria

Supervisor:					Co- Supervisor:

Professor E.B. Babatunde          		Professor C. O. Oluwafemi

Department of Physics,                                  Department of Physics,

Covenant University, Ota.                              Covenant University, Ota

Ogun State                                                      Ogun State

JULY 2007

CERTIFICATION

Chidi Chukwuemeka Uhuegbu, a postgraduate student in the Department of Physics with registration number CU03GP0037 has satisfactorily completed the requirements in research work for the degree of Doctor of Philosophy in physics with emphasis on solar energy physics.

The work embodied in this thesis is original and has not been submitted in part or full, thereof for any other diploma or degree or professional qualification of this or any other University.

---------------------------------                                                 --------------------------------------

Professor E.B. Babatunde                                                    Professor C. O. Oluwafemi

Department of Physics                                                         Head of Department of Physics

Covenant University                                                            Covenant University

DEDICATION

All to the Most High God.

ACKNOWLEDGEMENTS

First, I appreciate God Almighty for life, strength and protection throughout the period of this programme.

I express my sincere gratitude and appreciation to my supervisor professor E.B. Babatunde who brought his wealth of experience to see to the successful completion of this work. My gratitude goes to my Co-supervisor and Head, Department of Physics professor C.O. Oluwafemi and  to Professor M.A. Mesubi for his love and concern. I am eternally indebted for their guidance, encouragement, discussions and instructions.

I acknowledge all the contributions of my colleagues and friends who are too numerous to be listed.

My appreciation also goes to the following: The Chancellor, Dr David Oyedepo, members of the Board of Regent and Covenant University Ota Management for the opportunity to participate in the Staff Development programme. To members of my family: Mrs S.I. Uhuegbu, my beloved wife and lovely children: Chukwuemeka, Kosisochi and Chioma Uhuegbu for their patience and understanding, and to my parents, parents-law and my siblings I remain grateful.

My special thanks go to the following :  Dr Ayo C.K.,  Adekoya J. A.,  Ezeokonkwo C.N,  William A.B., Mrs Obi  C,  Dr Ezema  F.I,  Ayara W, Ekong V. E, Ikhu-Omoregbe N. Osamor V, Farojoye G. O, all members of the Department of Physics, Covenant University and to many others  whose names can not be mentioned here due to lack of space.

TABLE OF CONTENTS

Title………………………………………………………………………………………………ii

Certification……………………………………………………………………………………...iii

Dedication………………………………………………………………………………………..iv

Acknowledgement………………………………………………………………………………...v

Table of Contents…………………………………………………………………………….vi-xiii

List of Figures ..………………………………….…………………………………………xiv-xvi

List of Plates……………………………………………………………………………………xvii

List of Slides…………………………………………………………………………………...xviii

List of Set Ups …………………………………………………………………………………xvii

Abstract……………………………………………………………………………………xviii-xix

CHAPTER ONE

1.1.0     Introduction……………………………………………………………………………..1

1.2.0    Benefits of Thin Films…………………………………………………………………...2

1.3.0    Aim and Objectives of the Study….………………………………………………….3-4

CHAPTER TWO

2.1.0    Optical and Solid State Properties of Thin Film….………………………………………5

2.1.1   Transmittance……………………………………………………………………………5-6

2.1.2   Absorbance………………………………………………………………………………...6

2.1.3    Reflectance……………………………………………………………………………….7

2.1.4   Absorption Coefficient…………………………………………………………………..7-8

2.1.5   Optical Density……………………………………..…………………………...………8-9

2.2.0    Band gap and Absorption Edge…………………….………………………………..9-12

2.2.1 Absorption Edge  ……………………………………………………………...……12-13

2.2.2   Optical Constants……………………………………………………………………13-14

2.2.3   Dielectric Constant…………………………………………………….……………14-15

2.2.4   Optical Conductivity……………………………………………………………………15

2.2.5   Extinction Coefficient Factor………………………………………………………….15

2.3.0    Dispersion……………….………………………………………………………….15-16

2.4.0   Photoconductivity…….……………………………………………………………..16-17

2.5.0   Luminescence……….………………………………………………………………17-18

2.6.0   Electrical Conductivity….……………………………………………………………18

2.7.0 Thermal Conductivity………………………………………………………………...18-19

2.8.0    Spectral Selective Surfaces Aspect of Solar Energy Application………..…………..19

2.8.1 Spectral Selectivity……………………………………………………….…………...19-20

2.8.2 Solar Spectral Selective Absorber Surfaces………………………………..………...20-21

2.8.3 Semiconductor-Metal tandems……………..…………………………………………..21

2.8.4   Heat Mirrors…………………………………………………………………………21-22

2.8.5    Dark Mirrors……………………………………………………………………..…..22

2.8.6   Antireflection Coatings……………………………………………………………..22-23

2.8.7   Spectral Splitting and Cold Mirror Coatings………………………………………....23

2.8.8   Radiative Cooling Materials…………………………………………………………23

2.8.9   Window Coatings…………………………………………………………………..23-24

2.9.0   Solar Control Coatings………………………………………………………………24

2.9.1    Low Thermal Transmittance………………………………………………..………24

2.9.2 Materials for Solar Control and Low Thermal Transmittance…..…………………..24-25

2.9.3   Window Coatings with Dynamic Properties………………………………..…........25-26

CHAPTER THREE

3.0     Methods for Thin Film Growth ….………………………………………………….27

3.1.1     Thermal Evaporation….…………………………………………………………27-29

3.1.2     Epitaxial Growth….……………………………………………………………..29-30

3.1.2.1   Molecular Beam Epitaxial (MBE)……………………………………………...30-32

3.1.2.2 Liquid Phase Epitaxy ……………………………………………………………32

3.1.3   Sputtering……………………………………………………………………..…..32-34

3.1.4   Chemical Vapour Deposition (CVD)……………………………………………34-36

3.1.5    Spray Pyrolysis ………………………………………………………………….37

3.1.6     Plasma Technique………………………………………………………………37-38

3.1.7    Sol-gel Thin Film Formation…..………………………………………………...38

3.1.8   Precursor Sol…………..…………………………………………………………38-39

3.1.8.1   Sol-gel Dip Coating…………………………………………………………….39

3.1.8.2   Spin Coating…………………………………………………………………..39-40

3.1.8.3   Spin Deposition of Halide and Chalcogenide Films………………………….40-41

3.1.9      The Solution Growth Technique………………………………………….…..41-44

3.1.9.1    Thin Film Condensation Formation Mechanism……………………….…….44-45

3.1.9.2    Doping by Chemical Bath Deposition………………………………..………...45

CHAPTER FOUR

The Measurement Techniques of Thin Film Characteristics and Materials……………..46

4.1.0    Measurement Techniques of Thin Film Characteristics………………………….46

4.1.1      Film Thickness………………………………………………..………………...46

4.1.1.1    Micro balance (gravimetric ) Technique…..………………………………… ..47

4.1.1.2    Optical Technique……………………………………………………………...47-48

4.1.2      Absorbance/Transmittance Measurement………………………………………48

4.1.3      Method of Determining the Composition of Thin Films…………………….…48-49

4.1.3.1    Atomic Absorption Spectroscopic (AAS) Method………………………….....49

4.1.3.2    X-ray Fluorescence…………………………………………………………….49-50

4.1.3.3    Infrared Spectroscopy…………………………………………………………50-51

4.1.3.4    Qualitative and Quantitative Chemical Analysis (QCA)………………………52

4.2.0     Structural Characterization………………………………………………………52-53

4.2.1    Crystallographic Structure and Topography……………………………………...53-54

4.2.1    Transmission Electron Microscopy (TEM)………………………………………53-54

4.2.2    Surface Structure…………………………………………………………………54

4.2.2.1   LEED Technique…………………………..…………………………………...54

4.2.2.2    RHEED Technique…………………………………………………………….54-55

4.2.2.3    Photo Electron Spectroscopy (PES) …………………………………………...55

4.2.2.4     Optical Microscopy…………………………………………………………...55-56

4.3.0    Methodology……………………...……………………………………………...57-58

4.3.1    Iron Copper Sulphide...…………………………………………………………..58-60

4.3.2    Optical and Solid State Characterization…………………………………………60

4.3.3    Film Thickness Measurement……………………………………………………60-61

4.4.   Morphological Analysis…………………………………………………...……...…61

CHAPTER FIVE

5.0   Results and Observations……………………………………………………….……62

5.1   Optical Properties of Iron Copper Sulphide (FeCuS)………………………….….…..62

5.1.1   Absorbance (A) ……………………………………………………………………..62

5.1.2   Transmittance (T) …………………………………………………………………...62

5.1.3    Reflectance (R ) ………………………………………………………………........62-63

5.1.4    Absorption Coefficient ( α ) ………………………………………………………..63

5.1.5    Refractive Index (n) …………………………………………………………………63

5.1.6    Optical Conductivity (σo ) …………………………………………………………..64

5.1.7     Extinction Coefficient ( k) …………………………………………………………64

5.2        Solid State Properties……………………………………………………………….64

5.2.1     Band gap Energy (Eg) ……………………………………………………………....64-65

5.2.2    Dielectric Constant (real part) (ε r ) …………………………………………………65

5.2.3     Dielectric Constant ( imaginary part ) (ε i ) ………………………………………..65

5.3        Optical Properties of Iron Zinc Sulphide (FeZnS)…………………………………65

5.3.1      Absorbance (A) …………………………………………………………………...65

5.3.2       Transmittance (T) ………………………………………………………………...66

5.3.3        Reflectance (R) ………………………………………………………………….66

5.3.4        Absorption Coefficient (α ) ……………………………………………………...66

5.3.5       Refractive Index (n) ………………………………………………………………66-67

5.3.6       Optical Conductivity (σo) …………………………………………………………67

5.3.7      Extinction Coefficient ( k) ………………………………………………………...67

5.4         Solid State Properties………………………………………………………………67

5.4.1      Band gap Energy ( Eg)………………………………………………………………67

5.4.2      Dielectric Constant (real ) (ε r) ………………………………………………….....68

5.4.3       Dielectric Constant (imaginary part ) (ε i )………………………………………...68

5.5         Optical Properties of Lead Silver Sulphide ( PbAgS)……………………………..68

5.5.1       Absorbance (A) .…………………………………………………………………..68

5.5.2       Transmittance ( T )………………………………………………………………..69

5.5.3      Reflectance ( R ) …………………………………………………………………..69

5.5.4       Absorption Coefficient  (α ) ……………………………………………………...69

5.5.5        Refractive Index ( n) …………………………………………………………….69-70

5.5.6      Optical Conductivity (σo ) ……………………………………………………...…70

5.5.7        Extinction Coefficient ( k ) ……………………………………………………...70

5.6           Solid State Properties……………………………………………………………..71

5.6.1        Band gap Energy ( Eg ) …………………………………………………………..71

5.6.2       Dielectric Constant (real part ) (ε r ) ………………………………………….......71

5.6.3        Dielectric Constant ( imaginary part ) (ε i )…………………………………........71-72

5.7            Optical Properties of Copper Silver Sulphide (CuAgS)………………………....72

5.7.1         Absorbance (A) ………………………………………………………………….72

5.7.2          Transmittance ( T ) ……………………………………………………………..72

5.7.3            Reflectance ( R ) ……………………………………………………………...72

5.7.4           Absorption Coefficient (α ) ……………………………………………………73

5.7.5           Refractive Index (n ) …………………………………………………………..73

5.7.6          Optical Conductivity (σo ) ……………………………………………………...73

5.7.7          Extinction Coefficient ( k) ……………………………………………………..73

5.8             Solid State Properties …………………………………………………………..73

5.8.1          Band gap Enegry ( Eg ) …………………………………………………………73-74

5.8.2          Dielectric Constant (real part ) (ε r) …………………………………………….74

5.8.3          Dielectric Constant (imaginary part ) (ε i )……………………………………...74

5.9            Optical Properties of Copper Zinc Sulphide (CuZnS)…………………………..74

5.9.1          Absorbance ( A ) ……………………………………………………………….74

5.9.2          Transmittance ( T ) ……………………………………………………………..75

5.9.3          Reflectance ( R ) …………………………………………………………….….75

5.9.4         Absorption Coefficient (α ) …………………………………………………..…75-76

5.9.5          Refractive Index ( n) …………………………………………………………...76

5.9.6          Optical Conductivity (σo) ………………………………………………………76

5.9.7          Extinction Coefficient ( k ) ……………….……………………………………77

5.10           Solid State Properties…………………………………………………………...77

5.10.1      Band gap Energy ( Eg) ………………………………………………………..…77-78

5.10.2       Dielectric Constant (real part ) (ε r ) …………………………………………….78

5.10.3      Dielectric Constant ( imaginary part ) (ε i ) ………………………………………78

CHAPTER SIX

6.0 Analysis and Discussion……………………………………………………………..….80

6.1 The Spectral Analysis...…………………………………………………………………80

6.2 Other Optical Properties…………………………………………………………………80

6.3 Solid State Properties…………………………………………………………………….80-81

CHAPTER SEVEN

Conclusion and Recommendations ………………………………………………………..82

7.0 Conclusion………………………………………………………………………………..82-84

7.1 Recommendation………………………………………………………………………….85

REFERENCES……………………………………………………………………………...86-99

Appendix A. Figures……………………………………………………………………….100-154

Appendix B  Plates………...………………………………………………………………155-157

Appendix C Slides…………………………………………………………………………158-159

Appendix D Set Ups ………………………………………………………………………160-161

LIST OF FIGURES

Figure 5.1 Graph of absorbance (A) versus wavelength for FeCuS thin film………………..100

Figure 5.2 Graph of transmittance (T) versus wavelength for FeCuS thin film……………...101

Figure 5.3 Graph of reflectance (R) versus wavelength for FeCuS thin film………………...102

Figure 5.4 Graph of absorption coefficient versus photon energy for FeCuS thin film……...103

Figure 5.5 Graph of refractive index versus photon energy for FeCuS thin film…………….104

Figure 5.6 Graph of optical conductivity versus photon energy for FeCuS  thin film……….105

Figure 5.7 Graph of extinction coefficient versus photon energy for FeCuS thin film………106

Figure 5.8 Graph of α2 versus photon energy for FeCuS thin film……….………………….107

Figure 5.9 Graph of α1/2 versus photon energy for FeCuS thin film…………………............108

Figure 5.10 Graph of dielectric constant (real part) versus photon energy for FeCuS thin film.109

Figure 5.11 Graph of dielectric constant (imaginary part) versus photon energy for FeCuS thin film……………………………………………………………………………………………...110

Figure 5.12 Graph of absorbance (A) versus wavelength for FeZnS thin film………………...111

Figure 5.13 Graph of transmittance (T) versus wavelength for FeZnS thin film………………112

Figure 5.14 Graph of reflectance (R ) versus wavelength for FeZnS thin film………………..113

Figure 5.15 Graph of absorption coefficient versus photon energy for FeZnS thin film………114

Figure 5.16 Graph of refractive index versus photon energy for FeZnS thin film……………..115

Figure 5.17 Graph of optical conductivity versus photon energy for FeZnS thin film………...116

Figure 5.18 Graph of extinction coefficient versus photon energy for FeZnS thin film……….117

Figure 5.19 Graph of α2 versus photon energy for FeZnS thin film…...………………….........118

Figure 5.20 Graph of α1/2 versus photon energy for FeZnS thin film...………………………...119

Figure 5.21 Graph of dielectric constant (real part) versus photon energy for FeZnS thin film.120

Figure 5.22 Graph of dielectric constant (imaginary part) versus photon energy for FeZnS thin film……………………………………………………………………………………………...121

Figure 5.23 Graph of absorbance (A) versus wavelength for PbAgS thin film………………...122

Figure 5.24 Graph of transmittance (T) versus wavelength for PbAgS thin film…………........123

Figure 5.25 Graph of reflectance (R ) versus wavelength for PbAgS thin film……………......124

Figure 5.26 Graph of absorption coefficient versus photon energy for PbAgS thin film………125

Figure 5.27 Graph of refractive index versus photon energy for PbAgS thin film……………126

Figure 5.28 Graph of optical conductivity versus photon energy for PbAgS thin film………127

Figure 5.29 Graph of extinction coefficient versus photon energy for PbAgS thin film……..128

Figure 5.30 Graph of α2 versus photon energy for PbAgS thin film………………………….129

Figure 5.31 Graph of α1/2 versus photon energy for PbAgS thin film…………………………130

Figure 5.32 Graph of dielectric constant (real part) versus photon energy for PbAgS thin film.131

Figure 5.33 Graph of dielectric constant (imaginary part) versus photon energy for PbAgS thin film……………………………………………………………………………………………...132

Figure 5.34 Graph of absorbance (A) versus wavelength for CuAgS thin film……………......133

Figure 5.35 Graph of transmittance (T) versus wavelength for CuAgS thin film……………...134

Figure 5.36 Graph of reflectance (R ) versus wavelength for CuAgS thin film……………......135

Figure 5.37 Graph of absorption coefficient versus photon energy for CuAgS thin film……...136

Figure 5.38 Graph of refractive index versus photon energy for CuAgS thin film…………….137

Figure 5.39 Graph of optical conductivity versus photon energy for CuAgS thin film……......138

Figure 5.40 Graph of extinction coefficient versus photon energy for CuAgS thin film………139

Figure 5.41 Graph of α2 versus photon energy for CuAgS thin film…………………………...140

Figure 5.42 Graph of α1/2 versus photon energy for CuAgS thin film……………….................141

Figure 5.43 Graph of dielectric constant (real part) versus photon energy for CuAgS thin film…………………………………………………………………………………..…………142

Figure 5.44 Graph of dielectric constant (imaginary part) versus photon energy for CuAgS thin film……………………………………………………………………………………………..143

Figure 5.45 Graph of absorbance (A) versus wavelength for CuZnS thin film………………..144

Figure 5.46 Graph of transmittance versus wavelength for CuZnS thin film……………….....145

Figure 5.47 Graph of reflectance (R ) versus wavelength for CuZnS thin film……………......146

Figure 5.48 Graph of absorption coefficient versus photon energy for CuZnS thin film………147

Figure 5.49 Graph of refractive index versus photon energy for CuZnS thin film…………….148

Figure 5.50 Graph of optical conductivity versus photon energy for CuZnS thin film………..149

Figure 5.51 Graph of extinction coefficient versus photon energy for CuZnS thin film………150

Figure 5.52 Graph of α2 versus photon energy for CuZnS thin film…………………………...151

Figure 5.53 Graph of α1/2 versus photon energy for CuZnS thin film………………….............152

Figure 5.54 Graph of dielectric constant (real part) versus photon energy for CuZnS thin film.153

Figure 5.55 Graph of dielectric constant (imaginary part) versus photon energy for CuZnS thin film……………………………………………………………………………………………...154

LIST OF PLATES

Plate 5.1 Photomicrograph of FeCuS…………………………………………………………..155

Plate 5.2 Photomicrograph of FeZnS…………………………………………………………..156

Plate 5.3 Photomicrograph of PbAgS…………………………………………………………..156

Plate 5.4 Photomicrograph of CuAgS…………………………………………………………..157

Plate 5.5 Photomicrograph of CuZnS…………………………………………………………..157

LIST OF SLIDES

Slide 5.1 Picture of FeCuS thin film…………………………………………………………..158

Slide 5.2 Picture of FeZnS thin film…………………………………………………………..158

Slide 5.3 Picture of PbAgS thin film…………………………………………………………..159

Slide 5.4 Picture of CuAgS thin film…………………………………………………………..159

Slide 5.5 Picture of CuZnS thin film…………………………………………………………..159

LIST OF SET UPS

Set Up 3.1 Experimental Set Up ……………………………………………………………....160

Set up 4.1 Flow Chart for the Growth Process ……….………………………...……………..161

ABSTRACT

Ternary thin films of Iron Copper Sulphide (FeCuS), Iron Zinc Sulphide (FeZnS), Lead Silver Sulphide (PbAgS), Copper Silver Sulphide (CuAgS) and Copper Zinc Sulphide (CuZnS) were grown using cheap and simple solution growth technique with EDTA, TEA and NH3 as complexing agents. The deposited films were characterized using PYE-UNICO-UV-2102 PC spectrophotometer, and optical microscopy. The results suggest that some of the films have crystal structures. From the spectral analysis of absorbance/transmittance, the optical and solid state properties were deduced. The other optical properties so obtained include the reflectance, absorption coefficient, refractive index, extinction coefficient, optical conductivity and thickness, while the solid state properties are dielectric constant and band gap energy.

For all the five categories of thin films grown (i.e. FeCuS, FeZnS, PbAgS, CuAgS and CuZnS), absorbance was high in UV and low in VIS-NIR-regions, while the transmittance were low in UV-region and high in VIS-NIR-regions. The reflectances were high in UV-region and low in the VIS-NIR-regions.

For FeCuS, FeZnS, PbAgS, CuAgS and CuZnS, the absorption coefficient ranged from 0.1x106 m-1 to 1.65x106 m-1, 0.2x106 m-1 to 2.3x106 m-1, 0.5x106 m-1 to 0.9x106 m-1, 0.5x106 m-1 to 1.28x106 m-1 and 0.24x106 m-1 to 1.6x106 m-1, respectively. The real part of the refractive index ranged from 1.2 to 2.3, 0.72 to 2.3, 0.1 to 2.3, 1.94 to 2.28 and 1.6 to 2.3, respectively. The corresponding values of optical conductivity ranged from 0.03x1014 s-1 to 0.6x1014 s-1, 0.07x1014 s-1, 0.06x1014 s-1 to 0.6x1014 s-1, 0.24x1014 s-1 to 0.6x1014 s-1 and 0.12x1014 s-1 to 0.6x1014 s-1, respectively. The extinction coefficient, ranged from 0.005 to 0.038, 0.004 to 0.056, 0.010 to 0.140, 0.025 to 0.064 and 0.008 to 0.082, respectively. The direct band gap ranged from 2.4eV to2.8eV for FeCuS, 2.9eV for FeZnS, 1.5eV to 2.1eV for PbAgS, 2.3eV for CuAgS and 2.2eV to 2.4eV for CuZnS. The values of the indirect band gap were in the range 0.6eV to 1.0eV for FeCuS, 1.9eV for FeZnS, 0.3eV to 0.8eV for PbAgS, 1.1eV for CuAgS and 0.4eV to 0.9eV for CuZnS. The real part of the dielectric constant ranged from 1.4 to 5.2, 0.7 to 5.2, 0.4 to 5.2, 3.8 to 5.2 and 2.2 to 5.2, respectively, while the corresponding imaginary part of the dielectric constant ranged from 0.008 to 0.136, 0.008 to 0.164, 0.010 to 0.390, 0.100 to 0.290 and 0.030 to 0.360, respectively.

The range of band gaps, 1.5eV to 2.9eV makes the films suitable for solar cells fabrication; this is in agreement with the finding for the film FeCdS.